## Slide 1
unique raw materials × innovation
Refractories for the cement industry
for avant-garde quality

## Slide 2
contents
1
who we are
2
what we offer
3
how we work
Russian Magnezit
avant-grade quality
universal RMAG product line
integrated approach
key advantages of our solutions
unique equipment
advanced technology
innovative products
RMAG Standard category
RMAG Top category
RMAG High category
Magnezit Group
geography
development
modernization program

## Slide 3
1
experience × inspiration
who we are
for achievements

## Slide 4
1. who we are
An international vertically integrated company with Russian roots
our competencies
production and distribution of refractory materials
innovation-driven engineering and comprehensive services for thermal vessels
production and distribution of materials based on magnesite and other own raw materials
our advantages
founded in 1901
backbone enterprise in Satka monotown, Chelyabinsk Region
100% self-sufficiency in terms of raw materials for over 100 years down the line
full-cycle production
innovative products and solutions
coverage for all high potential global markets
a technological leader in the domestic industry
the number one manufacturer of magnesia-based refractories in Russia and the CIS
one of the largest refractory manufacturers worldwide
Magnezit Group

## Slide 5
geography
Russia
Extraction and production
Satka production site, Satka, Chelyabinsk Region — the company’s production centerpiece
Nizhne-Priangarsk production site, Razdolinsk – extraction and processing of unique Siberian magnesite
Service
Magnezit Montazh Servis, Satka
Trade representations
Moscow, Saint Petersburg, Chelyabinsk, Magnitogorsk, Ekaterinburg, Novokuznetsk, Orsk, Nizhny Tagil, Nizhny Novgorod, Krasnoyarsk, Taganrog
Worldwide
Extraction and production
Slovmag a.s., Lubenik, Slovakia
Liaoning Dalmond Refractories, Yingkou, Laobian District, China
Service
Magref, Ukraine
Aziya-Ogneupor, Kazakhstan
Distribution*
Magnezit Group Europe, worldwide
Dalmond Trade House, worldwide
TIMAB Magnesium, EU
Traxys, USA
Mitsui, Japan
Magref, Ukraine
*Partners and distribution regions.
1. who we are

## Slide 6
modernization and innovation
resource saving and energy efficiency
environmental safety
constructive partnerships
social responsibility
Key focus areas of the Development Strategy up until
2025
development
1. who we are

## Slide 7
modernization and innovation
Boost qualitative shifts in production capacity and processes to deliver high-quality innovative products with high added value
resource saving and energy efficiency
environmental safety
constructive partnerships
social responsibility
development
1. who we are
Key focus areas of the Development Strategy up until
2025

## Slide 8
environmental safety
constructive partnerships
social responsibility
modernization and innovation
resource saving and energy efficiency
Ensure rational and efficient use of production resources (raw materials, energy, etc.) to reduce capital and material intensity for end products and improve labor productivity and product quality
1. who we are
development
Key focus areas of the Development Strategy up until
2025

## Slide 9
constructive partnerships
social responsibility
modernization and innovation
resource saving and energy efficiency
environmental safety
Minimize environmental impact and ensure top production safety levels to protect human life and health
1. who we are
development
Key focus areas of the Development Strategy up until
2025

## Slide 10
social responsibility
modernization and innovation
resource saving and energy efficiency
environmental safety
constructive partnerships
Build partnerships with all stakeholder groups based on the principles of good faith, honesty, mutual trust and respect, professionalism, sanctity of contract, and information transparency
1. who we are
development
Key focus areas of the Development Strategy up until
2025

## Slide 11
modernization and innovation
resource saving and energy efficiency
environmental safety
constructive partnerships
social responsibility
Respect the interests of employees, ensure decent working conditions and social and spiritual well-being in the community, and stimulate socio-economic development of regions where the company operates
1. who we are
development
Key focus areas of the Development Strategy up until
2025

## Slide 12
modernization program
objectives
strengthen the competitiveness of the Group’s products
increase production volumes
expand the product mix
introduce modern technology
automate and robotize processes
save resources and improve energy efficiency
minimize environmental impact
total investments under the Global Technological Modernization Program up until 2025
34
bn rubles
in green production and environmental initiatives
20%
The modernization program encompasses the entire production cycle and aims to stimulate innovation in key points of growth that determine not only our future but also the future of the entire industry.
Chart: 
| Строка1 | Строка2
Столбец2 | 80 | 20
1. who we are

## Slide 13
Russian Magnezit
Russian Magnezit is fused and dead-burned magnesia with an MgO content of up to
98,5%
produced from the unique Siberian magnesite via a double-step technology.
Russian Magnezit can be used for manufacturing a wide range of high-performance refractory products for thermal vessels required by various industries.
learn more
The modernization program enables the Group to attain a significant growth in production volumes for both Russian Magnezit and innovative derivative products.
Russian Magnezit fused magnesia
Russian Magnezit dead-burned magnesia
* Total output for Satka and Nizhne-Priangarsk production sites.
20 000 metric tons p.a.
5 000 metric tons p.a.
90 000 metric tons p.a.
50 000 metric tons p.a.
about the Russian Magnezit
1. who we are

## Slide 14
for avant-garde quality
2
unique raw materials × innovation
what we offer

## Slide 15
2. what we offer
avant-garde quality
Focus on cutting-edge Russian-made refractories for the cement industry
«We offer an innovative line of RMAG refractories for the cement industry based on a unique mineral filler – Russian Magnezit. Cutting-edge production equipment guarantees top quality of each piece».
Sergey Odegov general director, Magnezit Group
target results
for clients and partners
stable high quality of products
independence from market fluctuations and the global political climate
advancements in production

## Slide 16
unique equipment
The production line serving the needs of the cement industry is a part of Impulse, a modern production facility.
Unique features of the production line
40 000 tpa
100%
compliance with environmental standards
LAEIS hydraulic presses
ABB robot solutions
Riedhammer tunnel kiln
Omega Impulse 40
end-to-end line automation — from mixing to labeling and packaging.
optimized logistics with fully localized equipment.
uniform firing in an energy-efficient kiln.
external and internal defect control for each item.
minimizing the impact of the human factor.
2. what we offer
automatic sorting and packaging facility
how the production line works
production line for refractories for the cement industry
Location:
Satka production site, Impulse facility
Products:
magnesia-spinel refractories of various mixtures
Line capacity:
Commissioned in July 2021

## Slide 17
advanced technology
The automatic sorting and packaging facility is a joint creation of Magnezit Group and experts representing several foreign companies. All the processes, including analysis, sorting, labeling, and packaging for all items are integrated and fully automated to rule out the human factor.
how the sorting facility works
“The sorting and packaging facility installed on the production line serving the needs of the cement industry is one of its kind worldwide in terms of both the degree of automation and the depth of quality control.”
2. what we offer
Dmitry Borzov Development Director, Magnezit Group
Robotized automatic sorting and packaging facility

## Slide 18
advanced technology
Robotized automatic sorting and packaging facility
The automatic sorting and packaging facility is a joint creation of Magnezit Group and experts representing several foreign companies. All the processes, including analysis, sorting, labeling and packaging for all items are integrated and fully automated to rule out the human factor.
how the production line works
packaging
external and internal defect control in the test chamber for each item
internal defects analy-sis — ultrasonic testing
external parameter analysis: 48 visual parameters
clock speed — 4.9 se-conds per 1 item
continuous lab analysis
3 types of labeling continuously applied: thermal pads, color labeling, and coding
2 cameras used for labeling control
corrugated box and stretch wrap
cardboard layers added between every 2 rows
QR coding for each pallet
safety guaranteed for all delivery options
labeling
analysis and sorting
2. what we offer

## Slide 19
innovative products
Russian Magnezit, dead-burned magnesia, is used as the main mineral filler for RMAG products.
learn more about Russian Magnezit
RMAG categories have different levels of resistance to thermal, mechanical, and chemical loads.
RMAG Top
RMAG High
RMAG Standard
— extremely high and very high resistance
— high resistance
— standard resistance
2. what we offer

## Slide 20
RMAG Top
Fired magnesia-spinel products with extremely high and very high resistance to thermal, mechanical and chemical loads
Intended for dry kilns and can be used in extremely severe and very severe conditions.
innovative products
mixture specifics
dead-burned magnesia Russian Magnezit
fused alumina-magnesium spinel
low levels of impurity oxides
functional properties
high resistance to thermal loads
corrosion resistance
high abrasion resistance
high resistance to chipping
conditions of use
high levels of alkali oxides
highly corrosive environment
extremely high thermal loads
unstable coating
high abrasive wear
use of aggressive alternative fuel (AF)
2. what we offer
Product labeling example for RMAG T1 type/size B622

## Slide 21
Fired magnesia-spinel products with extremely high and very high resistance to thermal, mechanical, and chemical loads Intended for dry kilns and can be used in extremely severe and very severe conditions
Physical properties and chemical analysis | RMAG-Т1 | RMAG-Т11 | RMAG-Т2 | RMAG-Т21 | RMAG-Т3 | RMAG-Т31 | RMAG-Т1Z | RMAG-Т2Z
Content, % |  |  |  |  |  |  |  | 
MgO | 86.0 | 88.0 | 85.5 | 90.0 | 85.0 | 89.0 | 85.0 | 85.0
Al2O3 | 12.0 | 10.0 | 12.0 | 7.5 | 12.0 | 7.7 | 11.0 | 11.0
SiO2 | 0.4 | 0.4 | 0.5 | 0.5 | 0.6 | 0.6 | 0.4 | 0.5
CaO | 0.8 | 0.8 | 1.0 | 1.0 | 1.2 | 1.2 | 0.8 | 1.0
Fe2O3 | 0.7 | 0.7 | 0.8 | 0.8 | 0.8 | 0.8 | 0.7 | 0.8
ZrO2 | – | – | – | – | – | – | 1.8 | 0.5
Open porosity, % | 15.0 | 15.0 | 150 | 15.0 | 15.5 | 15.5 | 15.0 | 15.0
Сrushing strength, N/mm3 | 60 | 60 | 60 | 60 | 60 | 60 | 60 | 60
Refractoriness under load, °С (ISO 1893-89 in Т05) | 1 700 | 1 700 | 1 700 | 1 700 | 1 700 | 1 700 | 1 700 | 1 700
Thermal shock resistance, air, number of coolings (GOST R 52542-2006, EN 993-11) | 100 | 80 | 100 | 80 | 100 | 80 | 100 | 100
Thermal shock resistance, water, number of coolings (GOST 7875.0-2018, GOST 7875.1-2018) | 25 | 15 | 25 | 15 | 25 | 15 | 25 | 25
RMAG Top
The typical data represent results of testing samples in accordance with the valid standards. These values are not obligatory. We reserve the right for other technical development and related changes of product parameters.
2. what we offer
innovative products

## Slide 22
RMAG High
Fired magnesia-spinel products with high resistance to thermal, mechanical, and chemical loads
Intended for dry and wet kilns and can be used in severe conditions
functional properties
adequate coating reception capacity
highly elastic (flexible) structure
refractoriness
conditions of use
elevated levels of alkali oxides
high to moderate chemical loads
high mechanical and thermal loads
unstable coating
partial use of alternative fuel (AF)
mixture specifics
dead-burned magnesia Russian Magnezit
fused alumina-magnesium spinel
may additionally contain chrome ore
optimal levels of impurity oxides
2. what we offer
innovative products

## Slide 23
Fired magnesia-spinel products with high resistance to thermal, mechanical and chemical loads Intended for dry and wet kilns and can be used in severe conditions
Physical properties and chemical analysis | RMAG-Н1 | RMAG-Н11 | RMAG-H1C | RMAG-Н2 | RMAG-H2С
Content, % |  |  |  |  | 
MgO | 85.0 | 89.0 | 86.0 | 84.0 | 86.0
Al2O3 | 12.0 | 7.7 | 7.0 | 12.0 | 6.0
SiO2 | 0.7 | 0.7 | 0.8 | 0.8 | 1.0
CaO | 1.4 | 1.4 | 1.5 | 1.4 | 1.5
Fe2O3 | 0.9 | 0.9 | 2.0 | 1.0 | 3.0
ZrO2 | – | – | 2.1 | – | 2.4
Open porosity, % | 16.0 | 16.0 | 16 | 16 | 16
Сrushing strength, N/mm3 | 65 | 65 | 60 | 60 | 60
Refractoriness under load, °С (ISO 1893-89 in Т05) | 1 690 | 1 690 | 1 680 | 1 680 | 1 680
Thermal shock resistance, air, number of coolings (GOST R 52542-2006, EN 993-11) | 100 | 80 | 90 | 100 | 80
Thermal shock resistance, water, number of coolings (GOST 7875.0-2018, GOST 7875.1-2018) | 25 | 15 | 20 | 25 | 20
RMAG High
The typical data represent results of testing samples in accordance with the valid standards. These values are not obligatory. We reserve the right for other technical development and related changes of product parameters.
2. what we offer
innovative products

## Slide 24
RMAG Standard
Fired magnesia-spinel products with standard resistance to thermal, mechanical and chemical loads
Mainly intended for wet kilns and some areas of dry kilns under normal operating conditions
functional properties
coating holding capacity
moderate refractoriness and resistance to mechanical loads
conditions of use
stable environment
standard thermal loads
moderate mechanical loads
mixture specifics
dead-burned magnesia
dead-burned magnesia Russian Magnezit
fused alumina-magnesium spinel
optimal levels of impurity oxides
2. what we offer
innovative products

## Slide 25
Fired magnesia-spinel products with standard resistance to thermal, mechanical, and chemical loads Mainly intended for wet kilns and some areas of dry kilns under normal operating conditions
Physical properties and chemical analysis | RMAG-S1 | RMAG-S2 | RMAG-S3
Content, % |  |  | 
MgO | 85.0 | 84.0 | 84.0
Al2O3 | 11.0 | 11.0 | 10.0
SiO2 | 1.0 | 1.5 | 1.7
CaO | 1.5 | 1.9 | 2.0
Fe2O3 | 1.3 | 1.5 | 2.0
Open porosity, % | 16.0 | 16.0 | 17.0
Сrushing strength, N/mm3 | 60 | 55 | 55
Refractoriness under load, °С (ISO 1893-89 in Т05) | 1 670 | 1 640 | 1 560
Thermal shock resistance, air, number of coolings (GOST R 52542-2006, EN 993-11) | 90 | 80 | 80
Thermal shock resistance, water, number of coolings (GOST 7875.0-2018, GOST 7875.1-2018) | 20 | 15 | 15
RMAG Standard
The typical data represent results of testing samples in accordance with the valid standards. These values are not obligatory. We reserve the right for other technical development and related changes of product parameters.
2. what we offer
innovative products

## Slide 26
experience × inspiration
for achievements
3
how we work

## Slide 27
in-house production
engineering
service
logistics
recycling
3. how we work
integrated approach
We possess a full range of competencies to offer an integrated approach to addressing our customers’ needs.

## Slide 28
We possess a full range of competencies to offer an integrated approach to addressing our customers’ needs.
3. how we work
integrated approach
in-house production
engineering
RMAG refractories
shotcrete and filling mixtures for rotary kilns, cyclone preheaters, decarbonizers, grate coolers, burners, and other units
metal and ceramic anchors
block-based items
service
logistics
recycling

## Slide 29
We possess a full range of competencies to offer an integrated approach to addressing our customers’ needs.
integrated approach
service
logistics
recycling
in-house production
engineering
modernization of thermal vessels and production lines and design of new ones
custom design of linings and metal structures for thermal vessels
3D models of thermal vessels
thermal and strength analysis of thermal vessel structures using the ANSYS software
3. how we work

## Slide 30
We possess a full range of competencies to offer an integrated approach to addressing our customers’ needs.
integrated approach
logistics
recycling
in-house production
engineering
service
field supervision at the stage of lining installation works with due regard to the customer’s requirements
end-to-end monitoring of refractory works, lining condition, parameters, and operating modes
provision of auxiliary equipment for lining installation and maintenance
training courses for technical staff
a full range of refractory works, including provision of the necessary equipment
3. how we work

## Slide 31
We possess a full range of competencies to offer an integrated approach to addressing our customers’ needs.
integrated approach
recycling
in-house production
engineering
logistics
a unique packaging system ensuring maximum protection during transshipment and storage
delivery by any transport to any location worldwide
service
3. how we work

## Slide 32
We possess a full range of competencies to offer an integrated approach to addressing our customers’ needs.
integrated approach
in-house production
engineering
recycling
a recycling program for used linings and their reuse for various needs
service
logistics
3. how we work

## Slide 33
key advantages of our solutions
based on RMAG products for the cement industry
quality assurance
We run quality checks for each item
stable supplies
We use our own raw materials to manufacture products at our own plants
lining durability
We offer products with minimum porosity and gas permeability, maximum refractoriness and structural flexibility
rational solutions
We can help you find the right product, mixture, and properties for each lining
production efficiency
We strive to minimize unit costs for end products and reduce market volatility risks
green processes
Our products will help you extend the life cycle of your thermal vessels and reduce your environmental impact
3. how we work

## Slide 34
Magnezit Group website
thank you
vustinov@magnezit.com
info@magnezit.com
msk@magnezit.com
(495) 232-61-00
Representation in Moscow: Bolshaya Polyanka St., Bldg. 3, Moscow, Russia, 119180